## Slide 1: Evaluating the Scalability of the Sonication Method of Graphene oxide Synthesis
Evan Dexter

## Slide 2: Graphene
Single or few layers of carbon atoms
200 times stronger than steel
High thermal conductivity
No band gap – extremely low electrical resistance
Magnetic properties
Catalyst
Very hard to make in large amounts

## Slide 3: Synthesis
Mechanical Exfoliation
Chemical Vapor Deposition
Sonication (Liquid-Phase Exfoliation)

## Slide 4: Previous research
Lots of researchers interested in graphene
  Effect of graphite concentration
  Surfactant choice and concentration
  Thermal effects
  Vessel geometry
  Sonication time with non-oxidative synthesis
  Sonication volume with non-oxidative synthesis

## Slide 5: question
How does sonication volume and time affect the synthesis of graphene oxide?
How does this translate to synthesis on a production scale?

## Slide 6: setup

## Slide 7: Sonication
Ultrasonic wave energy bombarding suspended particles
VirTis VirSonic 475

## Slide 8: SONication

## Slide 9: Centrifugation
Forces leftover non-graphene material to bottom of solution

## Slide 10: drying

## Slide 11: Experimental Factor levels
Sonication Volume
  100mL, 200mL, 500mL, 1000mL
Sonication Time
  1 hour, 2 hours, 3 hours, 4 hours
16 Possible combinations of factor levels

## Slide 12: Detection / Quantification
Raman Spectroscopy
Shows Purity, Thickness
Not Available at Olivet - University of Louisville
Higher D/G ratio indicates sheet defects
2D peak is symmetric and sharp for fewer layers
Raman Spectroscopy Example

## Slide 13: Research challenges
Not all factor levels tested
Raman spectroscopy results
Completed Experimental Trials |  |  |  | 
Sonication Time Factor (minutes) | Sonication Volume Factor (mL) |  |  | 
 | 100 | 200 | 500 | 1000
60 | Completed | Completed | - | -
120 | Completed | Completed | Completed | -
180 | Completed | - | - | -
240 | - | - | - | -

## Slide 14: results
Sonication Volume (mL) | Sonication Time (minutes) | Product Collected (grams) | Extrapolated Product (grams) | Percent Yield (%) | Rate of Production (grams · L-1 · min-1)
100 | 60 | 0.335 | 0.419 | 20.9 | 0.0698
100 | 120 | 0.422 | 0.528 | 26.4 | 0.0440
100 | 180 | 0.261 | 0.326 | 16.3 | 0.0181
200 | 60 | 0.234 | 0.585 | 14.6 | 0.0488
200 | 120 | 0.225 | 0.563 | 14.1 | 0.0234
500 | 120 | 0.370 | 2.313 | 23.1 | 0.0385

## Slide 15: results
Chart: Overall Production Rate by Sonication Volume
| 100 | 100 | 100 | 200 | 200 | 500
 | 0.069792 | 0.043958 | 0.018125 | 0.04875 | 0.023438 | 0.038542
Chart: Overall Production Rate by Sonication Time
| 60 | 120 | 180 | 60 | 120 | 120
 | 0.069792 | 0.043958 | 0.018125 | 0.04875 | 0.023438 | 0.038542

## Slide 16: conclusions
Rate of synthesis can be sustained at higher sonication volumes
Increasing volumes do not require longer sonication times
Liquid sonication is a promising method for future graphene oxide synthesis
Additional research suggested at larger scales

## Slide 17: acknowledgements
Mentoring/Advising
  Dr. John Tatarko
  Dr. Daniel Sharda
Assistance/Logistics
  ONU Dept. of Chemistry
  Dr. Greg Long
  Dr. Willa Harper
  Dr. Gamini Sumanasekera – University of Louisville
Funding
  Olivet Honors Program

## Slide 18: Thank you!
Questions?