## Slide 1: Survey of the Performance of 5 nm Gold Nanoparticles Within an ssDNA-Stabilized Biosensor for the Detection of Hg2+
Madalyn Zagajowski
Mentored by Dr. Bruce Heyen

## Slide 2: Purpose and Background 1

## Slide 3: Mercury(Hg)
Mercury is a neurotoxin, with exposure leading to irreversible and possibly fatal consequences.
Acute exposure symptoms
  neurological damage, seizures, vomiting, diarrhea, necrosis of the gut mucosa
Chronic exposure symptoms
  Fatigue, tremors, memory loss, neurological damage, personality changes, delirium, hallucinations

## Slide 4: Environmental Accumulation
            Industrialization has caused mercury to accumulate in the environment (Hg2+)
                -Minamata Bay, Japan
                -California mines
            Knowing mercury is present is necessary to prevent mercury poisoning cases
https://coastalreview.org/wp-content/uploads/2012/05/Fish-Contaminated-with-Methylmercury.jpg
https://apjjf.org/data/553-2.jpg

## Slide 5: How can we detect mercury?
Mercury is a fluorescence quencher
The indicator must be fluorescent and selective to mercury
https://www.researchgate.net/profile/Alexandros-Katranidis/publication/333495332/figure/fig5/AS:765955672141824@1559629471157/Fluorescence-quenching-of-EmGFP-in-the-presence-of-different-concentrations-of-mercury.ppm

## Slide 6: Selectivity: Thymine
https://pubs.acs.org/cms/10.1021/ja056354d/asset/images/medium/ja056354dn00001.gif
One of the four nucleotide bases found in DNA
Mercury spontaneously binds to up to two thymine bases and forms T-Hg-T dimers
Single-stranded DNA (ssDNA) that possesses all thymine will be very selective to mercury

## Slide 7: Fluorescence: Gold Nanoparticles (AuNPs)
Particles of gold a few hundred/thousand atoms big
Can be stabilized with a variety of molecules, including many biochemicals
Can be used as a fluorescence source
https://www.mdpi.com/applsci/applsci-10-03824/article_deploy/html/images/applsci-10-03824-g001.png

## Slide 9: How the biosensor is used
Poly(30)T ssDNA strands are mixed into water sample, and Hg binds with it
AuNPs are introduced, allowing for the ssDNA to interact with them
Spectroscopy is used to analyze the sample (UV-vis and fluorescence)

## Slide 10: Main Obstacle
DNA and AuNPs are both overall negatively charged, so they won’t interact spontaneously.
  Usually worked around by using thiolated DNA strands, however this requires cleaving a disulfide bond to make the thiol groups first
  This process requires extra equipment and is somewhat time-consuming

## Slide 11: A Possible Method
Yang et. al. developed a method for binding that does not require thiolated DNA
ssDNA can stabilize smaller AuNPs (around 5 nm diameter) without thiol groups
Using this method for a biosensor may not produce a detectable/quantifiable fluorescence signal due to AuNP size

## Slide 12: Research Question
Will the Yang method produce a biosensor that can produce a noticable, consistent, and quanitfiable fluorescence signal that indicates mercury presence?

## Slide 13: Methodology 2

## Slide 14: Methodology
Synthesis of
5 nm AuNPs
Preparation of Hg-bound ssDNA
Preparation of samples
Spectroscopicanalysis
1
2
3
4

## Slide 15: Synthesis of AuNPs
Chloroauric acid solution and sodium citrate solution were mixed
  HAuCl4: 10 mL, 1 mM
  Sodium citrate: 0.8 mL, 38.8 mM
Sodium borohydride solution (0.3 mL, 0.1 M) was added dropwise
AuNP hydrosol was aged for 24 hours

## Slide 16: Preparation of Hg-bound ssDNA
Poly(30)T ssDNA solution was mixed with HgCl2 for each sample
  ssDNA: 15 μL, 10 μM
  HgCl2 : 15 μL, 10 μM
Incubated at 37°C for 30 minutes, followed by addition of 8 U exonuclease I and incubation for an additional 30 minutes

## Slide 17: Preparation of samples for spectroscopy
1 mL aliquots to be analyzed by spectroscopy were prepared and incubated for at least 3 hours
  10 μL of AuNP hydrosol
  60 μL of ssDNA, either Hg-bound or non-Hg-bound
  930 μL of HEPES buffer (0.1 M, pH 7.0)

## Slide 18: Spectroscopic analysis
UV-vis spectroscopy – Shimadzu UV-1280 spectrophotometer
  To learn the peak absorbance wavelength
  To look for a red shift in the absorbance
Fluorescence spectroscopy – Hitachi F-2500 spectrophotometer
  To look for significant fluorescence peaks within a certain range
  To look for a trend in the difference between the peaks

## Slide 19: Results and Discussion 3

## Slide 20: Fluorescence Data
One significant peak at 791 nm present in all AuNP-ssDNA complex samples
General trend of Hg-bound samples having a lower peak – however some samples did not exhibit the trend
Sample type | No mercury bound | Mercury bound
Fluorescence Intensity | 4.94 | 3.777 ± 0.71
Wavelength (nm) | 790.7 | 790.8 ± 0.29

## Slide 21: Discussions: Fluorescence Data
Nature of the peaks at 791 nm
  A bit far from the excitation wavelength of 518 nm
  Small intensity
  Ratio of intensity of Hg-bound AuNPs to non-Hg-bound AuNPs close to 1
No other peaks found
  Fluorescence signal too small to be easily detected
  AuNPs may be too small

## Slide 22: UV-vis Data
Red shift observed for all Hg-bound samples, but only one of the non-Hg-bound samples
Absorbance is much lower for Hg-bound samples
Sample type | Control (no DNA) | No mercury bound | Mercury bound
Absorbance | 0.302 | 0.344 ± 0.0087 | 0.160 ± 0.0059
Wavelength (nm) | 517.4 | 518.04 ± 0.30 | 524.1 ± 0.81

## Slide 23: Discussions: UV-vis Data
Lack of red shift in the non-Hg-bound complexes
  Complex didn’t form?
  Unclear - more experimenting needed
Lower absorbance exhibited by Hg-bound complexes
  Shadowing – exonuclease I

## Slide 24: Conclusion 4

## Slide 25
From the data obtained, the Yang method did not produce a biosensor that may easily and accurately indicate the presence of mercury in a water sample by fluorometric analysis.
The size of the AuNPs may have compromised the biosensor’s abilities.
Size of the peak
Variation in the intensity for the same concentration of Hg2+
Possibility of shadowing

## Slide 26: Future Work
Further confirmation of the AuNP-ssDNA complex formation
  Polyacrylamide gel electrophoresis (PAGE)
  Transmission electron microscopy (TEM) imaging
https://blogs.imperial.ac.uk/fonsmad2015-velox/files/2015/07/Gold-Nanoparticles.jpg
https://noteshippo.com/wp-content/uploads/2021/06/SDS-PAGE-principle-and-Protocol.webp

## Slide 27: Future Work
Greater number of samples for analysis
Experimentation with concentrations of sample constituents
Mercury concentrations of different amounts

## Slide 28: References
Environmental Health Department, Ministry of the Environment. Minamata Disease: The History and Measures. Tokyo, Japan: Ministry of the Environment, Government of Japan; 2002.
Ali, H., Khan, E., & Ilahi, I. (2019). Environmental Chemistry and Ecotoxicology of Hazardous Heavy Metals: Environmental Persistence, Toxicity, and Bioaccumulation. Journal of Chemistry. 6730305.
Alpers, C. N., Hunerlach, M. P., May, J. T., & Hothem, R. L. (2005). Mercury Contamination from Historical Gold Mining in California. U.S. Geological Survey. 2005-3014.
Bernhoft R. A. (2012). Mercury toxicity and treatment: a review of the literature. Journal of Environmental and Public Health. 460508.
Chen, J., Ji, X., Tinnefeld, P., & He, Z. (2015). Multifunctional Dumbbell-Shaped DNA-Templated Selective Formation of Fluorescent Silver Nanoclusters or Copper Nanoparticles for Sensitive Detection of Biomolecules. ACS Appl. Mater. Interfaces. 8, 1786– 1794.
He, H., Xie, C., & Ren, J. (2008). Nonbleaching Fluorescence of Gold Nanoparticles and Its Applications in Cancer Cell Imaging. Analytical Chemistry, 80(15), 5951–5957.
Jiang, P., Wang, Y., Zhao, L., Ji, C., Chen, D., & Nie, L. (2018). Applications of Gold Nanoparticles in Non-Optical Biosensors. Nanomaterials (Basel). 8(12), 977.
Khoshbin, Z., Housaindokht, M.R., Verdian, A., & Bozorgmehr, M.R. (2018). Simultaneous detection and determination of mercury (II) and lead (II) ions through the achievement of novel functional nucleic acid-based biosensors. Biosensors and Bioelectronics. 116, 130-147.

## Slide 29: References
Li, J., Fu, W., Bao, J., Wang, Z, & Dai, Z. (2018). Fluorescence Regulation of Copper Nanoclusters via DNA Template Manipulation toward Design of a High Signal-to-Noise Ratio Biosensor. ACS Appl. Mater. Interfaces. 10(8), 6965–6971.
Liu, B. & Liu, J. (2017). Methods for preparing DNA-functionalized gold nanoparticles, a key reagent of bioanalytical chemistry. Anal. Methods. 9, 2633.
Millward, G.E., Turner, A., & He, X. (2019). Metal pollution. Encyclopedia of Ocean Sciences (3rd ed.). Elsevier Science & Technology.
Park, K.S., Jung, C., & Park, H.G. (2010). “Illusionary” Polymerase Activity Triggered by Metal Ions: Use for Molecular Logic-Gate Operations. Angewandte Chemie International Edition. 49(50), 9757-9760.
Qing, Z., Bai, A., Xing, S., Zou, Z., He, X., Wang, K., & Yang, R. (2019). Progress in biosensor based on DNA-templated copper nanoparticles. Biosensors and Bioelectronics. 137, 96-109.
Yang, J., Lee, J.Y., Too, H.P., Chow, G.M., & Gan, L.M. (2006). Single stranded DNA stabilization and assembly of Au nanoparticles of different sizes. Chemical Physics. 323(2), 304–312.
Yang, M., Chen, X., Su, Y., Liu, H., Zhang, H., Li, X., & Xu, W. (2020). The Fluorescent Palette of DNA-Templated Silver Nanoclusters for Biological Applications. Front. Chem. 8, 601621.

## Slide 30: Questions?